Horizontal Foam Seal - A WBAsicsTM Product by Watson Bowman Acme

# Pre-compressed, Monolithic Cross Section Foam Supported, Silicone Faced Expansion Joint System

A.	General

The work shall consist of furnishing, placing and bonding a pre-compressed, monolithic cross section foam supported, silicone faced expansion joint system in accordance with the details shown on the plans and the requirements of these specifications.  Components of the system shall not be substituted and shall be supplied from one Expansion Joint Manufacturer.

Expansion Joint Manufacturer shall have a minimum ten (10) years’ experience specializing in the design and supply of silicone and foam expansion joint systems and technologies.

- Quality Control

Manufacturer shall be ISO-900 certified to the current edition and shall provide written confirmation that a formal Quality Management System and Quality Processes have been adopted in the areas of, including but not limited to, Engineering, Manufacturing, Quality Control and Customer Service for all processes, products and their components.  Alternate Manufacturers will be considered provided they submit written proof that they are ISO 9001 certified to the current edition prior to the project bid date.

# C.	Product

Provide a pre-compressed, monolithic cross section foam supported, silicone faced expansion joint system that is capable of accommodating movements of +/-60% of joint opening and as shown in the contract plans. The expansion joint system shall be comprised of a hydrophobic 100% acrylic impregnated polyurethane, monolithic cross section foam seal coated with a highway grade silicone.

The system shall be bonded in place by a two component 100% solids epoxy adhesive.

Horizontal Foam Seal - A WBAsicsTM Product by Watson Bowman Acme

Pre-compressed, Monolithic Cross Section Foam Supported, Silicone Faced Expansion Joint System

# D.	Component and Materials

The Contractor shall furnish a Manufacturer’s certification that the materials proposed shall meet the requirements as set forth in the specification.

- Joint Seal Profile

The silicone faced system shall be supported by a pre-compressed, hydrophobic acrylic impregnated foam seal manufactured without any vertical or horizontal laminations.  Material composition shall be free of any waxes or wax compounds; asphalts or asphalt compounds meeting the following physical requirements

| PHYSICAL PROPERTIES | TEST METHOD | REQUIREMENT |
| --- | --- | --- |
| Elongation at break | ASTM D3575; Suffix: T | 125% +/-20% |
| Tensile Strength, psi (kPa) | ASTM D3575; Suffix: T | 21 psi min |
| UV / Light & Moisture Resistance | DIN 18542 | Pass |
| Density | ASTM D545 | 4-6lb./cu. ft |
| Impregnation | N/A | Proprietary, modified, water-based, acrylic |
| Compression Set | ASTM D 3574 | 3% max |

Horizontal Foam Seal - A WBAsicsTM Product by Watson Bowman Acme

Pre-compressed, Monolithic Cross Section Foam Supported, Silicone Faced Expansion Joint System

Adhesive

System shall be supplied with a two-component low modulus, 100% solids, general purpose epoxy gel that meets ASTM-C881, Type III, Grade: 3, Class: B&C. Epoxy shall have uses in patching, bonding, and surface sealing building materials, and satisfy the physical properties listed in the table below:

bonding, and surface sealing.

.

| PHYSICAL PROPERTIES | ASTM METHOD | REQUIREMENTS |
| --- | --- | --- |
| Blended Color | Visual | Gray Concrete |
| Tensile Strength | ASTM D638 | 2,400 psi (17 Mpa) |
| Flexural Strength | ASTM D790 | 500 psi (3 Mpa) |
| Bond Strength (48 hrs) | ASTM C321 | 575 psi (4 Mpa) |
| Water Absorption | N/A | 0.3% (24hrs) |
| Pot Life (3oz) @ 77F | N/A | 45 min. |

### E.	Construction Requirements

The Contractor shall submit product information and necessary details after the award of the contract.  At the discretion of the Engineer, the Manufacturer may be required to furnish a representative sample of material to be supplied in accordance with these specifications.

The contractor shall ensure system and components are stored per Manufacturer’s recommendations, and properly prepare all joint interfaces prior to installation in accordance with the manufacturer’s installation guidelines. Repair joint interfaces where needed and with materials approved by the Expansion Joint Manufacturer.

All joint interfaces must be completely dry prior to application of the expansion joint system. Pre-compressed foam supported, silicone faced expansion joint system shall be sized in accordance with Manufacturer’s recommendations and installed at locations shown on the contract plans. Accommodations for adjacent construction temperature shall be considered when sizing the seal. Install the foam supported, silicone faced seal per Manufacturer’s installation guidelines to ensure complete contact with joint interface and silicone faced seal profile.

Position the silicone faced seal to the proper depth and leave end of profile up to properly splice adjoining seal if applicable.

Horizontal Foam Seal - A WBAsicsTM Product by Watson Bowman Acme

Pre-compressed, Monolithic Cross Section Foam Supported, Silicone Faced Expansion Joint System

### F. Payment

The accepted quantity of pre-compressed monolithic foam supported, silicone faced expansion joint system will be paid for at the contract unit price per lineal foot.  Measurement shall be taken horizontally along the centerline of the joint system between the outer limits indicated on the contract plans.

Payment will be made under:

PAY ITEM						PAY UNIT

# Pre-compressed Foam Supported

# Silicone Faced Expansion Joint System		Lineal Foot

Payment will be full compensation for all work necessary to complete the items including furnishing and installing the joint seal, and any miscellaneous patching required.