PRODUCT INFORMATION

Manufacturer:	   Watson Bowman Acme Corp.

95 Pineview Drive

Amherst, NY 14228

(P) 800-677- 4922

(F) 716-691-9239

www.wbacorp.com

Product Name     Wabo®CreteSPS Joint System

Product

Description:  	Wabo®CreteSPS Joint System is an expansion joint system which bonds a preformed silicone seal to concrete, steel, elastomeric concrete or viscoelastic concrete joint interface with a silicone adhesive

Intended Use:       To seal expansion joints on bridges

A.	General

The work shall consist of furnishing, placing and bonding a preformed silicone joint seal with a silicone adhesive to adjacent structures in accordance with the details shown on the plans and the requirements of these specifications.  Components of the preformed silicone joint sealing system shall not be substituted and shall be supplied from one expansion joint manufacturer.

Expansion Joint Manufacturer shall have a minimum ten (10) years experience specializing in the design and manufacture of silicone technology expansion joint systems.

By additionally adding Wabo Crete:

The work shall consist of furnishing and installing an elastomeric concrete material in accordance with the details shown on the plans and the requirements of the specifications.

- Quality Control

Expansion Joint Manufacturer shall be ISO-9001and RC-14001 certified, and shall provide written confirmation that a formal Quality Management System has been independently audited and approved to these standards.  Alternate manufacturers will be considered provided they submit written proof that they are ISO 9001 and RC 14001 certified prior to the project bid date.

# C.	Product

Provide a preformed silicone joint sealing system that is capable of accommodating movements as shown in the contract plans. The preformed silicone joint seal shall be manufactured from extrusion grade organic silicone compound, and preformed by an extruding process.

Provide a field mixed elastomeric concrete header material. The elastomeric concrete material shall be field mixed and consist of a two component elastomer and pregraded aggregate mix.

The preformed silicone seal shall be bonded to the joint interface with a silicone adhesive and without the use of any primers

# D.	Component and Materials

The Contractor shall furnish the selected expansion joint manufacturer’s certificate of compliance that materials proposed will meet the requirements as set forth in these specifications

- Preformed Silicone Seal

Preformed silicone seal shall be manufactured of an extrusion grade, custom organic silicone compound meeting the following physical requirements.  Alternative elastomeric materials are not allowed.

| PHYSICAL PROPERTY | TEST METHOD | REQUIRMENTS |
| --- | --- | --- |
| Color | Visual | Gray |
| Durometer (Shore A) | ASTM D 2240 | 55+/- 5 |
| Tensile Strength | ASTM D 412 | 1000 psi, min |
| Elongation | ASTM D 412 | 400% min |
| Tear Resistance (die B) | ASTM D 624 | 100 lbs/in min |
| Compression Set @ 350 o F, 22 hrs | ASTM D 395 | 30% max |

- Silicone Adhesive

The adhesive shall be medium modulus, neutral cure sealant manufactured of silicone meeting the following physical properties.

| PHYSICAL PROPERTY | TEST METHOD | REQUIRMENTS |
| --- | --- | --- |
| Color | Visual | Gray |
| Durometer (Shore A) | ASTM D2240 | 25 +/- 5 |
| Elongation | ASTM D412 | 700% min |
| Tensile at 100% Elongation | ASTM C1184 | 70 psi, min |
| Peel Adhesion to substrates | ASTM C 794 | 55 lbs/in min |
| Work Life (tool time) |  | 20 -30 minutes |

3. Silicone Sealant Adhesive

The 2 Part silicone adhesive shall be medium modulus, neutral cure sealant manufactured of silicone meeting the following physical properties.

| PHYSICAL PROPERTY | TEST METHOD | REQUIRMENTS |
| --- | --- | --- |
| Color | Visual | Gray |
| Durometer (Shore A) | ASTM D2240 | 25 +/- 5 |
| Elongation | ASTM D412 | 700% min |
| Tensile at 100% Elongation | ASTM C1184 | 70 psi, min |
| Peel Adhesion to substrates | ASTM C 794 | 55 lbs/in min |
| Work Life (tool time) |  | 20 -30 minutes |

The Contractor shall furnish a manufacturer’s certification that the materials proposed have been pre-tested and will meet the requirements as set forth in the specification.

- Elastomeric Concrete

Material shall be an ambient cure, 100% solids, two component polyurethane with pregraded aggregate mix exhibiting the physical properties listed in the tables below. When properly mixed and poured, the elastomeric concrete cures rapidly, flows and fills any voids, spalls or irregularities forming a monolithic unit.

Elastomeric cured binder shall meet the following physical properties:

| PHYSICAL PROPERTY | TEST METHOD | REQUIRMENTS |
| --- | --- | --- |
| Tensile strength | ASTM D638 | 750 min., psi |
| Elongation @ break | ASTM D638 | 150 % |
| Hardness, Durometer D | ASTM D2240 | 30-49 |
| Compression Set, 22 hr @ 158 °F | ASTM D395 Method B | 50 % max |
| Tear Resistance, min, lb/in | ASTM D 624 | 80 |
| Water Absorbtion | ASTM D570 | 3% max |
| Heat Shrinkage, % | ASTM D1299 | 1.6 max |
| Oven Aging @ 158°F For 72 hr - tensile | ASTM D638 | 750 |
| Elongation | ASTM D638 | 150% min |

Elastomeric cured binder and aggregate shall meet the following physical properties:

| PHYSICAL PROPERTY | TEST METHOD | REQUIRMENTS |
| --- | --- | --- |
| Compressive Strength | ASTM D695 | 2200 psi min |
| Resilience @ 5% deflection | ASTM D695 | 90% min |
| Slant Shear Bond Strength to concrete |  | 250 psi min. |
| Impact Resistance | ASTM D3029 |  |
| @ 32°F (0°C) |  | No cracks |
| @ -20°F (29°C) |  | No cracks |
| @158°F (70°C) |  | No cracks |

- Bonding Agent

Provide manufacturers two component, 100% solids bonding agent. Apply bonding agent to the sides and base of the preformed concrete blockout prior to placement of the elastomeric concrete. Store, mix and apply in accordance with manufacturer’s system data sheet.

Liquid components shall be identified by the following information:

| Part A | Resin | Clear |
| --- | --- | --- |
| Part B | Activator | Tan |

### E.	Cyclic Testing of Silicone Bridge Joint Systems

The preformed silicone joint sealing system shall be pre-qualified through cyclic testing by an independent laboratory.  The cyclic testing procedure shall determine the durability of the preformed silicone joint sealing system after two hundred cycles in compression and tension.   Any defects, tears or bond failure will be cause for rejection.

A document signed by an independent, third party testing or inspection laboratory to verify testing will be basis of acceptance.

| CYCLIC LOADING TEST PROPERTIES | REQUIREMENT |
| --- | --- |
| Test sample Length | 2 foot sample |
| Number of Cycles | 200 cycles |
| Movement | +/- 1 ” (1“ compression , 1” tension) |
| Joint Opening | 2 inches |
| Joint Skew | 45 o |
| Temperature | 68 oF (20 oC) and -20 o F (- 29 oC) |

### F.	Construction Requirements

The Contractor shall submit product information and necessary details after the award of the contract.  At the discretion of the Engineer, the manufacturer may be required to furnish a representative sample of material to be supplied in accordance with these specifications.

Store all materials per manufacturer’s recommendations

The contractor shall ensure and properly prepare all joint interfaces prior to installation and in accordance with the manufacturer’s installation guidelines. Repair joint interfaces where needed and with materials approved by the expansion joint manufacturer.

All joint interfaces must be completely dry prior to application of the silicone adhesive. Install the preformed silicone joint seal in one continuous length. Prior to installation, clean the silicone seal profile using a solvent approved by the manufacturer. Apply the silicone adhesive per manufacturer’s installation guidelines to insure complete contact with joint interface and preformed silicone seal.

Position the silicone seal to the proper depth and apply silicone adhesive along each side of seal and fill per manufacturer’s installation guidelines.

Preformed silicone joint sealing system shall be sized in accordance with manufacturer’s recommendations, and installed at locations shown on the contract plans.

The manufacturer shall provide instructions for the proper installation of the elastomeric concrete. Any patching materials must be approved prior to use from the manufacturer.  Elastomeric concrete shall be installed at locations shown on the contract plans and in strict accordance with the manufacturers written instructions along with the advice of their qualified representative.

G.	Payment

The accepted quantity of preformed silicone joint sealing system will be paid for at the contract unit price per lineal foot. Elastomeric concrete will be paid for at the contract unit price per cubic foot. Measurement of the preformed silicone joint sealing system will be taken along the centerline of the joint system between the outer limits indicated on the contract plans.

Payment will be made under:

PAY ITEM			PAY UNIT

Preformed Silicone

Joint Sealing System	Lineal Foot

Elastomeric Concrete           Cubic Foot

Payment will be full compensation for all work necessary to complete the items including furnishing and installing the preformed silicone joint sealing system, the elastomeric concrete, and any miscellaneous patching.

LIMITED WARRANTY:

Watson Bowman Acme Corp. warrants that this product conforms to its current applicable specifications.  Watson Bowman Acme Corp. makes no other warranty, express or implied, including any WARRANTY OF MERCHANTABILITY OR WARRANTY OF FITNESS FOR A PARTICULAR PURPOSE.  The sole and exclusive remedy of Purchaser for any claim concerning this product, including, but not limited to, claims alleging breach of warranty, negligence, strict liability or otherwise, is the replacement of product or refund of the purchase price, at the sole option of Watson Bowman Acme Corp.  Any claims concerning this product shall be submitted in writing within one year of the delivery date of this product to Purchaser and any claims not presented within that period are waived by Purchaser.  In no event shall Watson Bowman Acme Corp. be liable for any special, incidental, consequential (includes loss of profits) or punitive damages.  Other warranties may be available when the product is installed by a factory trained installer.  Contact your local Watson Bowman Acme representative for details.  The data expressed herein is true and accurate to the best of our knowledge at the time published; it is, however, subject to change without notice.

Contact

Watson Bowman Acme Corp.  95 Pineview Drive, Amherst, NY 14228

phone:716-691-7566 / fax: 716-691-9239 / web site: http://www.wbacorp.com

WaboCreteSPS_0713