SPECIFICATION

Section 07900

Wabo®Crete Membrane System

#### MM/MX/ME Series Expansion Joint System

with Wabo®Crete Parking Series “Gray”

PART 1 - GENERAL

1.01	Work Included

A.	The work shall consist of furnishing and installing expansion joints in accordance with the details shown on the plans and the requirements of the specifications. The joints are proprietary designs utilizing extruded elastomeric seals, elastomeric headers and mounting plates. In the event of any discrepancy between the contract drawings and specifications, the specifications shall govern.

B.	Related Work

- Cast-in-place concrete

- Miscellaneous and ornamental metals

- Flashing and sheet metal

- Sealants and caulking

1.02	Submittals

A.	Standard Drawings - Submit typical expansion joint cross-section(s) indicating pertinent dimensioning, general construction, blockout dimensions and product data information. Approved Installers shall prepare and submit details of all special conditions to the manufacturer for review and approval prior to installation.

1.03	Product Delivery, Storage and Handling

- Deliver products in each manufacturer's original, intact, labeled containers, pallets or bundles and store under shelter in a dry location with temperatures above 40°F until installed. Store off the ground, protect from freezing, direct sun exposure in elevated temperatures and construction activities.

1.04	Acceptable Manufacturers

A.	All joints shall be as designed and manufactured by Watson Bowman Acme Corp., 95 Pineview Drive, Amherst, NY 14228

B.	Alternate manufacturers and their products will be considered, provided they meet the design concept and are produced of materials that are equal to or superior to those called for in the base product specification.

- Any proposed alternate systems must be submitted and receive approval 21 days prior to the bid.  All post bid submissions will not be considered. This submission shall be in accordance with MATERIALS AND SUBSTITIONS.

- Any manufacture wishing to submit for prior approval must provide the following:

- A working 6-inch sample of the proposed system with a letter describing how the system is considered superior to the specified system.

- A project proposal drawing illustrating the recommended alternate system installed in the application, specific to the project.

- Verifiable list of prior installations showing prior and successful experience with the proposed system.

- Any substitution products not adhering to all specification requirements within, will not be considered.

1.05	Quality Assurance

A.	Manufacturer: Shall be ISO-9001:2015 certified and shall provide written confirmation that a formal Quality Management System and Quality Processes have been adopted in the areas of, (but not limited to) engineering, manufacturing, quality control and customer service for all processes, products and their components. Alternate manufacturers will be considered provided they submit written proof that they are ISO 9001:2015 certified prior to the project bid date. Manufacturers in the process of obtaining certification will not be considered.

B.	Warranty: The expansion control system shall be warranted when installed by the manufacturer’s factory trained installer. Installation shall be in strict accordance with manufacturer’s technical specifications, details, installation instructions and general procedures in effect for normal intended usage and suitable applications under specific design movements and loading conditions.

C.	Manufacturer: Shall have a minimum ten (10) years experience specializing in the design and manufacture of expansion control systems.

D.	Products: Expansion control systems shall be installed with manufacturer’s blockout repair and infill materials.

E.	Application: The specified expansion control system(s) shall be installed by the manufacturer’s factory trained installer.

##### PART 2 - PRODUCT

2.01 	General

A.	Provide watertight expansion control system that is capable of accommodating multi-directional movement. System shall consist of preformed thermoplastic rubber profiles with integral side flanges typically cast into a preformed blockout by means of utilizing manufacturer’s ambient cure elastomeric header.

The thermoplastic rubber seal element shall be sized to accommodate the total range of movement as dictated by the specifier at each joint location. Sizing shall be made in such a way as to ensure that the elastomeric membrane seal will remain under a degree of compression throughout the full movement cycle. Where required, provide seal that accepts pedestrian traffic. The contractor will provide evidence utilizing manufacturer’s product data that the membrane seal will comply with this requirement.

Furnish Wabo®Crete Membrane - ME, MX or MM Series seal element at locations requiring water tightness as manufactured by Watson Bowman Acme Corp. and as indicated on drawings.

2.02	Components and Materials

A.	Thermoplastic Rubber Joint Seals (Elastomeric Seal)

Provide seal profile as specified and indicated in the contract drawings. Profile design shall incorporate integral side flanges exhibiting a pronounced serrated profile and factory punched holes that interlocks the profile into the elastomeric header material. Material shall meet the physical and performance properties indicated below:

| PHYSICAL PROPERTIES | ASTM TEST METHOD | REQUIREMENT |
| --- | --- | --- |
| Shore A Hardness | D-2240 | 63 |
| Tensile Strength, min | D-412 | 986 psi |
| Ultimate Elongation, min | D-412 | 570% |
| 100% Modulus | D-412 | 363psi |
| Compression Set, max 22 hrs @ 73deg F | D-395 | 17% |
| 70 hrs @ 257 deg F |  | 40% |

| PERFORMANCE PROPERTIES | TEST METHOD | REQUIREMENT |
| --- | --- | --- |
| Ozone Resistance | ASTM D-1171 | No Cracks |
| UV Resistance | SAE J1960 | Pass |
| Staining Resistance | ASTM D-925 | No Staining |
| Fatigue Resistance | ASTM D-1052 | 2 Million Cycles |

B.    	Elastomeric Concrete Header:  (Wabo®Crete Parking Series)

Material shall be an ambient cure, 100% solids, two component polyurethane with pregraded aggregate mix exhibiting the physical properties listed in the tables below.  When properly mixed and poured, the elastomeric concrete cures rapidly, flows and fills any voids, spalls or irregularities forming a monolithic unit.

Base Color: Gray

1.  Elastomeric cured binder and aggregate shall meet the following physical properties:

PHYSICAL PROPERTIES      ASTM METHOD       REQUIREMENTS          TEST RESULTS

Compressive Strength             D695 Mod                    2200                             2723 psi

Resilience at 5% deflection      D695                             90 (min.)                         96.7%

Adhesion to concrete:              C190

Dry Bond                                                  400                              451.3 psi

Wet Bond                                                  250                             353.9 psi

Impact Resistance                  Steel ball drop (.375” th. Disc / dry steel plate)

At  -20 deg F(-29C)                                         no cracks at 5 ft                7.0 ft-lbs

At   32 deg F (0C)                                            no cracks at 5 ft              10.0 ft-lbs

At 158 deg F (70C)                                          no cracks at 5 ft              10.0 ft-lbs

C.	Bonding Agent

Provide manufacturer’s two component, 100 percent solids bonding agent and apply to the sides and base of the preformed blockouts prior to placement of Wabo®Crete II elastomeric header. Store, mix and apply in accordance with manufacturer’s system data sheet.

Liquid components shall be identified by the following information:

Part A - Resin; Color:  Clear

Part B - Activator; Color:  Tan

D.	Accessories - Provide necessary and related parts including MasterSeal 940 broadcast aggregate, preformed or fabricated Wall Mount Plates with appropriate anchors and sealants where required for complete installation.

2.03		Fabrication

A.	Thermoplastic Rubber Membrane Seal - Ship in the longest practical continuous length in manufacturer’s standard shipping carton or on wooden pallets shrink wrapped.

B.	Joint Seal Directional Changes - At all horizontal changes in direction provide seals with factory heat welded splices such as 90° corners, tees and crosses. The seal shall extend a minimum of 2’-0” in each direction from the factory splice.

Only straight, butt splice connections shall be allowed on the jobsite following manufacturers written instructions utilizing specialty heat fusing equipment or the manufacturer specialty-splicing adhesive.

All factory and field fused connections shall incorporate bonding of the complete seal profile. This includes fusing of all internal and external web configurations.

C.	Elastomeric  Header - Activator packaged in one-half gallon containers (Part A), resin packaged in gallon containers (Part B), 60 pound containers of aggregate (Part C) and MasterSeal 940 (50 lb bags) shipped on wooden pallets, shrink wrapped.

D.	Wall Mount Plate (corner condition) - Fabricated or preformed metal profiles shall be shipped in standard 10 ft. lengths and shall be cut to length on jobsite where required.  Plates shall be miter cut in the field to conform to directional changes unless otherwise contracted with expansion joint manufacturer.

2.04	Finishes

A.	Thermoplastic Rubber Membrane Seal shall be supplied in standard color:  Black.

- Elastomeric Header base material shall be supplied in standard color: Gray.

- Elastomeric Header material after field application of MasterSeal 940 broadcast granules:  Gray-textured.

PART 3 - EXECUTION

3.01	INSTALLATION

A.	Preparation of the Work Area

1.	The contractor shall provide a properly formed, solid concrete blockout per the manufacturer and project requirements. Any edge or area in need of repair shall utilize one of the Watson Bowman Acme concrete repair materials to provide a solid and square blockout. Call Technical Support Services at (800) 677-4WBA (4922).

2.	The contractor shall clean the concrete blockout of all contaminants and impurities by sandblasting immediately prior to Wabo®Crete Membrane installation. Concrete form release agents, water repellents, laitance, surface dirt and rust, all old sealants and other surface treatments and protective coatings are examples of materials which must be removed from the blockout substrate surface in order to obtain the proper Wabo®Crete Parking Series elastomeric header bond.

3.	Areas adjacent to the joint must be masked with tape to assure neat, clean joint lines.

4.	The blockout area must be completely dry for the application of Wabo®Crete Parking Series elastomeric header. Concrete must be cured a minimum of 14 days prior to placement of Wabo®Crete.  Wabo®Bonding Agent must be applied to blockout just prior to placement of Wabo®Crete. When the use of patching compounds is required for blockout repair, follow manufacturer’s guidelines for the recommended cure times prior to placement of Wabo®Crete Parking Series elastomeric header.

5.	The blockouts must be made to the dimensions and elevations shown on the standard system drawings. Deviations from these dimensions will not be allowed without the written consent of Watson Bowman Acme.

6.	The membrane seal element shall be unpacked and laid in a relaxed position to relieve any temporary coiling from shipment packaging prior to placement, the winged flaps of the gland element shall be wiped with an acceptable non-petroleum solvent cleaner such as Xylol (Xylene).

- Mix all Wabo®Crete Parking Series components and install membrane system in strict accordance with most current manufacturers installation procedures.  Installing contractor shall confirm that they are in possession of the latest procedures prior to beginning work. Refer to website for current information.

3.02	CLEAN AND PROTECT

Protect Wabo®Crete Membrane System during construction. Heavy construction vehicles will not be permitted to cross the joint without specific and written permission by the Engineer. Sub sequential damage to the Membrane System shall be repaired at the contractor’s expense.