Wabo®Crete StripSeal Joint System

# Armored Joint and Elastomeric Concrete Expansion Joint System

### for Bridge & Highway Applications

A.	General

The work shall consist of fabricating, furnishing and installing a strip seal  joint sealing system with an elastomeric concrete header in accordance with the details shown on the plans and the requirements of the specifications.

Manufacturer shall a minimum ten (10) years experience specializing in the design and manufacture of expansion control systems

- Quality Control

Manufacturer shall be ISO-9001:2015 certified and shall provide written confirmation that a formal Quality management System and Quality Processes have been adopted in the areas of, (but not limited to) Engineering, Manufacturing, Quality Control and Customer Service for all processes, products and their components. Alternate manufacturers will be considered provided they submit written proof that they are ISO-9001:2015 certified prior to the project bid date.

The strip seal joint manufacturer shall have an AISC Simple Structure Category shop approval.

# C.	Product

Provide a watertight joint sealing system that is capable of accommodating multidirectional movements.  The strip seal joint sealing system shall consist of a heavy-duty extruded or machined shape cast into the structure by means of sinusoidal anchorage and a field mixed elastomeric concrete header. The steel shapes shall be designed to accept and mechanically lock a continuous non-reinforced elastomeric seal.  Provide seal profile that satisfies project requirements including movement and watertightness.  The elastomeric concrete material shall be field mixed and consist of a two component elastomer and pregraded aggregate mix. Install all components utilizing manufacturer’s bonding agent and recommended lubricant/adhesive for complete installation.

Wabo®Crete StripSeal Joint System

# Armored Joint and Elastomeric Concrete Expansion Joint System

### for Bridge & Highway Applications

# D.	Component and Materials

The Contractor shall furnish a manufacturer’s certification that the materials proposed have been pre-tested and will meet the requirements as set forth in the specification.

- Steel Extrusions or Shapes

Material utilized to produce shape suitable to mechanically lock elastomeric seal shall conform to properties of ASTM A36 or A588.  Profile shall have a minimum thickness of ¼” as measured from the internal locking mechanism cavity to the top surface of the steel shape and shall be capable of accommodating various horizontal conditions and service loads including HS-20 loading.

Steel shapes shall be monolithic with a machined retainer cavity.  Multiple components welded steel shapes and rolled steel, which is bent or crimped to achieve final shape, or seal retainer cavity will not be permitted.

- Sinusoidal Anchorage

Provide manufacturer’s continuous sinusoidal steel profile.  Material shall be a minimum 3/8” diameter and meet the requirements of ASTM A36

- Lubricant Adhesive

Elastomeric seal shall be installed utilizing a one part moisture curing polyurethane and aromatic hydrocarbon solvent mixture which complies with ASTM D4070.

- Elastomeric Seal

Material shall be a flexible, non-reinforced extruded neoprene compound exhibiting the physical properties listed in the table below.  All elastomeric seals shall incorporate a unique locking lug that mechanically snaps into a corresponding extrusion or machined shape cavity to ensure watertightness and proper joint performance.  The elastomeric seal shall be supplied and installed in one continuous length and meet the following properties:

Wabo®Crete StripSeal Joint System

# Armored Joint and Elastomeric Concrete Expansion Joint System

### for Bridge & Highway Applications

PHYSICAL PROPERTIES		TEST METHOD		REQUIREMENT

Tensile Strength			ASTM D412		2000 psi,

Elongation @ break			ASTM D412		250%, min

Hardness, Type A Durometer		ASTM D2240 Modified	55  +/-5 % points

Oven Aging 70 hrs @ 212°F		ASTM D573

Tensile Strength						20% loss max

Elongation							20% loss max

Hardness							0 to +10 points

Oil Swell, 70 hrs @ 104°F		ASTM D471		45%

Ozone Resistance, 70 hrs @ 104°F	ASTM D1149 Method B	No Cracks

20% strain, 300 pphm, in air

Low Temperature Stiffening		ASTM D2240		0 to +15 points

7 days @ 14°F

Hardness (Type A durometer)

Compression Set, 70 hrs @ 212°F	ASTM D395 Method B	40%

- Elastomeric Concrete

Material shall be an ambient cure, 100% solids, two component polyurethane with pregraded aggregate mix exhibiting the physical properties listed in the tables below.  When properly mixed and poured, the elastomeric concrete cures rapidly, flows and fills any voids, spalls or irregularities forming a monolithic unit.

Elastomeric cured binder shall meet the following physical properties:

PHYSICAL PROPERTIES		TEST METHOD		REQUIREMENT

Tensile strength				ASTM D638		750 min., psi

Elongation @ break			ASTM D638		200 %

Hardness, Durometer D			ASTM D2240		30-49

Compression Set, 22hr @ 158°F	ASTM D395 Method B	50 % max

Tear Resistance, min, lb/in		ASTM D624		80

Water Absorption 			ASTM D570		3% max

Heat shrinkage, %			ASTM D1299		1.6 max

Oven Aging @ 158°F			ASTM D638		750

For 72 hr – tensile

Elongation				ASTM D638		150% min

Wabo®Crete StripSeal Joint System

# Armored Joint and Elastomeric Concrete Expansion Joint System

### for Bridge & Highway Applications

Elastomeric cured binder and aggregate shall meet the following physical properties:

PHYSICAL PROPERTIES		TEST METHOD		REQUIREMENT

Compressive Strength			ASTM D695		2200 psi min.

Resilience @ 5% deflection		ASTM D695		90% min

Slant Shear Bond Strength 					250 psi min.

to concrete

Impact Resistance			See Note 1

@ 32°F (0°C)							no cracks

@ -20°F (-29°C)						no cracks

@158°F (70°C)						no cracks

NOTE 1 - Test specimen is a cast disk 2.5” in diameter and 0.375” thick.  Specimens are conditioned four hours at test temperatures.  A one pound steel ball is dropped onto the center of the specimen through a plastic tube from an initial height of five feet.  The drop height is increased by ½ foot intervals until the specimen cracks. Drop is made within ten seconds after removal of specimen from the exposure condition.

- Bonding Agent

Provide manufacturers two component, 100% solids bonding agent.  Apply bonding agent to the sides and base of the preformed concrete blockout prior to placement of the elastomeric concrete.  Store, mix and apply in accordance with manufacturer’s system data sheet.

Liquid components shall be identified by the following information:

Part A – Resin        	Color: Clear

Part B – Activator 	Color: Tan

- Accessories

Provide necessary and related parts including leveling devices for complete installation of the system.

Wabo®Crete StripSeal Joint System

# Armored Joint and Elastomeric Concrete Expansion Joint System

### for Bridge & Highway Applications

### E.       Construction Requirements

The Contractor shall submit product information and necessary shop drawings after the award of the contract.  At the discretion of the Engineer, the manufacturer may be required to furnish a representative sample of material to be supplied in accordance with the project specifications

Strip seal joint sealing systems shall be set to the proper width for the ambient temperature at the time of installation.  Properly align all steel extrusions and shapes prior to welding operations to ensure proper joint performance and watertightness.

The manufacturer instructions for the proper installation of the joint system shall be entered on the shop drawings.  Shop drawings, which lack manufacturer installation instruction, may be returned without approval. Strip seal joint sealing systems along with the elastomeric concrete shall be installed in strict accordance with the manufacturers written instructions along with the advice of their qualified representative.

### F.       Payment

The accepted quantity of strip seal joint sealing system will be paid for at the contract unit price per lineal foot and the elastomeric concrete will be paid for at the contract unit price per cubic foot.  Measurement of the joint system will be taken horizontally and vertically along the centerline of the joint system between the outer limits indicated on the contract plans.  Payment will be made under:

PAY ITEM					PAY UNIT

Strip Seal Joint Sealing System		Lineal Foot

Elastomeric Concrete				Cubic Foot

Payment will be full compensation for all work necessary to complete the items including furnishing and installing the strip seal joint sealing, elastomeric concrete and any miscellaneous patching required.