Wabo®ElastoFlex Joint System

# Continuous Membrane Sealing System

For bridge and Highway applications

A.	General

The work shall consist of fabricating, furnishing and installing a bridge deck joint sealing system in accordance with the details shown on the plans and the requirements of the specifications.

Manufacturer shall a minimum ten (10) years experience specializing in the design and manufacture of expansion control systems

- Quality Control

Manufacturer shall be ISO-9001:2015 certified and shall provide written confirmation that a formal Quality management System and Quality Processes have been adopted in the areas of, (but not limited to) Engineering, Manufacturing, Quality Control and Customer Service for all processes, products and their components. Alternate manufacturers will be considered provided they submit written proof that they are ISO 9001:2015 certified prior to the project bid date.

# C.	Product

Provide a watertight joint sealing system that is capable of accommodating the structures movement. The joint sealing system shall consist of rubber reinforced anchor blocks and a continuous sealing membrane gland cast into the structure by cast in place anchors. The rubber anchor blocks shall be designed to withstand traffic loads and mechanically lock a continuous reinforced elastomeric seal. The shape of the seal profile shall promote self-removal of foreign materials and that satisfy project requirements including movement and watertightness. Install all components utilizing manufacturer’s epoxy bedding compound and recommended sealants for complete installation.

# D.	Component and Materials

The Contractor shall furnish a manufacturer’s certification that the materials proposed have been pre-tested and will meet the requirements as set forth in the specification.

Wabo®ElastoFlex Joint System

# Continuous Membrane Sealing System

# for Bridge & Highway Applications

- Rubber Anchor Blocks

The 6’-0” molded anchor blocks shall be comprised of a formed steel shape suspended in an elastomeric material. The profile-riding surface shall have grooves to ensure skid resistance and shall be capable of accommodating traffic loads. Each anchor block shall be supplied with integrated bolt hole cavities and tongue and groove end connections.

The elastomer used to mold the rubber anchor blocks shall be manufactured of an ethylene propylene diene monomer (EPDM) meeting the following properties as called for in ASTM D2000:

PHYSICAL PROPERTIES		TEST METHOD		REQUIREMENT

Hardness, Type A Durometer		ASTM D2240		65 +/-5

Tensile Elongation			ASTM D412		1500 psi, min.

Elongation @ break			ASTM D412		250%, min.

Compression Set, 22 hrs @ 212°F	ASTM D395 Method B	35%, max

Low Temperature Brittleness		ASTM D2137 Method A	Pass @ -40°F

After 3 min. @ -40°F

Ozone Resistance, 70 hrs @ 104°F	ASTM D1149 Method B	No Cracks

20% strain, 1000 pphm

Oil deterioration 70 hrs @ 212°F	ASTM D471		120% volume

After immersion in ASTM Oil #3				increase max

Steel Section – The steel angle is formed from plate meeting ASTM A36

- Elastomeric Gland

The continuous molded fabric-reinforced EFL elastomeric gland shall be supplied and installed in one continuous length. The elastomer compound shall be manufactured of an ethylene propylene diene monomer (EPDM) meeting the properties as called for in the chart above. The EFJ elastomeric gland shall be supplied and installed in one continuous length. The elastomer compound shall be manufactured from Santoprene Rubber or manufacturer’s alternate material exhibiting a Shore A Hardness of 67 +/- 3.

PHYSICAL PROPERTIES		TEST METHOD		REQUIREMENT

Hardness, Type A Durometer		ASTM D2240		67 +/- 3

Tensile Elongation			ASTM D412		850 psi

Elongation @ break			ASTM D412		300%

100% Modulus 				ASTM D412		435 +/- 95 psi

Tension Set, average 			ASTM D412		10%

Tear Strength, average			ASTM D624		140 pli @ 73°F

58 pli @ 212°F

Compression Set, average 168 hrs	ASTM D395		23% @ 73°F

Brittle Point, average			ASTM D746		< -76°F

Requirements shown above reflect test results taken immediately following compound mixing.  Results may vary and are not indicative of product performance if specimens are skived from finished, molded parts.

Wabo®ElastoFlex Joint System

# Continuous Membrane Sealing System

# for Bridge & Highway Applications

- Bolt Cavity Sealant

Bolt hole cavities shall be filled using a two part polyurethane sealant that meets Federal Specification TT-S-00227E. Contractors to ensure that the anchor blocks are dry from moisture prior to placement of material.

- Edge Void Sealant

Edge voids shall be filled with a one part polyurethane sealant conforming to Federal Specification TT-S-00230C Type II Non-Sag. Contractor shall ensure that the anchor blocks are dry from moisture prior to placement of material.

- Bedding Compound

Apply edge void sealant as a bedding material to the blockout base prior to placement of the elastomeric gland.  Material shall be a one part polysulfide base synthetic rubber sealant conforming to Federal Specification TT-S-00230C Type II Non-Sag.

### E.	Construction Requirements

The Contractor shall submit product information and necessary shop drawings after the award of the contract. At the discretion of the Engineer, the manufacturer may be required to furnish a representative sample of material to be supplied in accordance with the project specifications

Then device shall be accurately set and securely supported at the correct grade and elevation and the correct joint opening as shown on the plans and on the shop drawings.

The manufacturer instructions for the proper installation of the joint system shall be entered on the shop drawings. Shop drawings, which lack manufacturer installation instruction, may be returned without approval.

### F.	Payment

The accepted quantity of bridge deck joint sealing system will be paid for at the contract unit price per lineal foot. Measurement of the bridge deck joint sealing system will be taken horizontally and vertically along the centerline of the joint system between the outer limits indicated on the contract plans. Payment will be made under:

PAY ITEM					PAY UNIT

Bridge Deck Joint Sealing System		Lineal Foot

Payment will be full compensation for all work necessary to complete the items including furnishing and installing the bridge deck joint sealing system.