Wabo®Evazote UV

# Low Density, Closed Cell, Cross-linked, Ethylene Vinyl Acetate Polyethylene Copolymer,         Nitrogen Blown Joint Seal

for Bridge & Highway Applications

A.	General

# The work shall consist of furnishing and installing a low density, closed cell, cross-linked, ethylene vinyl acetate polyethylene copolymer, nitrogen blown joint seal in accordance with the details shown on the plans and the requirements of the specifications.

Manufacturer shall have a minimum ten (10) years experience specializing in the design and manufacture of expansion control systems

- Quality Control

Manufacturer shall be ISO-9001:2015 certified and shall provide written confirmation that a formal Quality management System and Quality Processes have been adopted in the areas of, (but not limited to) Engineering, Manufacturing, Quality Control and Customer Service for all processes, products and their components.  Alternate manufacturers will be considered provided they submit written proof that they are ISO 9001:2015 certified prior to the project bid date.

# C.	Product

Provide a bridge joint seal that consists of a impermeable closed-cell, cross-linked, ethylene vinyl acetate, low density polyethylene copolymer, nitrogen blown resilient, nonextrudable foam material with a UV stabilizer.  Bridge joint seal shall be held in place by a two component 100% solids epoxy adhesive.  The design of the seal shall be capable of accommodating movement and variations in joint widths through compression and tension of its shape.  Grooves sidewalls shall be be 1/8” (3mm) wide by 1/8” deep (3mm) and spaced between ¼” (6mm) to ½” (13mm) apart and run along the entire length of the bond surfaces of the seal to ensure an effective and quality surface for adhesion.  Provide seal profile that satisfies project requirements including movement and watertightness. Install all components utilizing manufacturer’s recommended adhesive for complete installation.

Wabo®Evazote UV

# Low Density, Closed Cell, Cross-linked, Ethylene Vinyl Acetate Polyethylene Copolymer,         Nitrogen Blown Joint Seal

for Bridge & Highway Applications

# D.	Component and Materials

The Contractor shall furnish a manufacturer’s certification that the materials proposed will meet the requirements as set forth in the specification.

- Joint Seal Profile

The seals shall be manufactured of low density closed cell cross linked Ethylene Vinyl Acetate Polyethylene Copolymer nitrogen blown material exhibiting the physical properties listed in the table below:

| PHYSICAL PROPERTIES | TEST METHOD | REQUIREMENT |
| --- | --- | --- |
| Elongation at break | ASTM D3575; Suffix: T | 255% +/-25% |
| Tensile Strength, psi (kPa) | ASTM D3575; Suffix: T | 115 psi +/- 21% |
| Tear Resistance | ASTM D624 | 15.0 lbs/inch +/- 20% |
| Density | ASTM D3575; Suffix W, Method A | 2.7 – 3.2 |
| Water Absorption | ASTM D3575; Suffix L | 0.02 lbs/sf |
| Compression Recovery (% of original width) 22 hr @ 73 o F (23 o C) ½ hr recovery | AASHTO T42 50% | No deterioration |
| Weather / Deterioration | AASHTO T42 Accelerated Weathering | No deterioration |
| Compression Set 50% compression for 22 hours @ 73o F (23 o C) 2 hr recovery 50% compression for 22 hours @ 73 o F (23 o C) 24 hour recovery | ASTM D3575; Suffix: B | 10% set 9% set |
| Extrusion ( specimen compressed 60% of original thickness with 3 restrained sides) | ASTM D545 | Extrusion on free side does not exceed 0.25 inches (6.4mm) |

Wabo®Evazote UV

# Low Density, Closed Cell, Cross-linked, Ethylene Vinyl Acetate Polyethylene Copolymer,         Nitrogen Blown Joint Seal

for Bridge & Highway Applications

- Adhesive

Joint seal shall be installed utilizing a 100% solids two component moisture insensitive modified epoxy adhesive which meets ASTM C-881 Type I & II Grade 2 Class B & C and  the requirements of the properties listed below:

Properties (uncured):

|  | Part A | Part B | Mixed |
| --- | --- | --- | --- |
| Color: | White | Carmel | beige |
| Shelf Life | 2 Years | 2 Years |  |
| Mixing ratio (By Vol) | 3 | 1 | 3:1 |
| Specifc Gravity | 1.47 | 1.15 |  |
| Density (lbs/gal) @ 77 o F (25 o C) | 12.2 +/-0.2 | 9.6 +/-0.2 | 1.6 +/-0.2 |
| Viscosity (cps) @ 77 o F (25 o C) | 22,000 | 33,000 | 26,000 |
| Pot Life (200 gms) |  |  | 32-36 minutes |
| Initial Set @ 77 o F |  |  | 1 ½ - 2 Hours |
| Initial Cure |  |  | 8-12 hours |
| Full Chemical Cure |  |  | 7 days |

Properties after Cure:

| TEST | TEST METHOD | REQUIREMENT |
| --- | --- | --- |
| Compressive Strength | ASTM D695 | 7000 psi |
| Tensile Strength | ASTM D638 | 3500 psi |
| Elongation at Break | ASTM D638 | 3-5% |
| Shore D hardness | ASTM D2250 | 75 |
| Water Absorption | ASTM D570 | 0.25% |
| Bond Strength | ASTM C-882 | 430 psi |

Wabo®Evazote UV

# Low Density, Closed Cell, Cross-linked, Ethylene Vinyl Acetate Polyethylene Copolymer,         Nitrogen Blown Joint Seal

for Bridge & Highway Applications

### E.	Construction Requirements

The Contractor shall submit product information and necessary details after the award of the contract.  At the discretion of the Engineer, the manufacturer may be required to furnish a representative sample of material to be supplied in accordance with the project specifications.  Where indicated and noted on the contract plans, install bridge joint seals in a neat and workmanlike manner.  All surfaces to receive bridge deck joint seal shall be free from dirt, water and any other loose foreign debris, which may be detrimental to effective joint sealing.

Measure the joint opening width.  Seal material should be sized 25% larger than the joint opening at near neutral but never less than 10% oversized or greater than 35% oversized.  The seal profile shall be cut to the correct length for installation. Care should be taken to extend the profile to its full length, without exerting any tension or stretching of the seal.

The bond at the splice location is achieved by heat welding. Heatwelds and splices and other  directional changes should be cut and made prior to seal installation.

Bridge deck joint seal shall be installed in strict accordance with the manufacturers written instructions.

### F.       Payment

The accepted quantity of bridge joint seal will be paid for at the contract unit price per lineal foot.  Measurement of the bridge joint seal will be taken horizontally and vertically along the centerline of the joint system between the outer limits indicated on the contract plans.

Payment will be made under:

PAY ITEM						PAY UNIT

# Low Density, Closed Cell, Cross-linked,

# Ethylene Vinyl Acetate Polyethylene Copolymer

# Nitrogen Blown Joint Seal				Lineal Foot

Payment will be full compensation for all work necessary to complete the items including furnishing and installing the bridge joint seal, and any miscellaneous patching required.