SPECIFICATION

Section 07900/079500

Wabo®InverSeal

Horizontal and Vertical

Expansion Control Systems

PART 1 - GENERAL

1.01	Work Included

A.	This work shall consist of furnishing and installing a deck joint sealing expansion control system at the location shown on the plans, and in accordance with the following specification.  The sealing system shall prevent the passage of water through the expansion joint opening.

B.	Related Work

- Cast-in-place concrete

- Flashing and sheet metal

- Sealants and caulking

1.02	Submittals

A.	Template Drawings - Submit typical expansion joint cross-section(s) indicating pertinent dimensioning and relationship to adjacent construction.

1.03	Product Delivery, Storage and Handling

A.	Deliver products in manufacturer's original, intact, labeled containers and store under cover in a dry location until installed.  Store off the ground, protect from weather and construction activities.

1.04	Acceptable Manufacturers

A.	All joints shall be as designed and manufactured by Watson Bowman Acme Corp., 95 Pineview Drive, Amherst, NY 14228

B.	Alternate manufacturers and their products will be considered, provided they meet the design concept and are produced of materials that are equal to or superior to those called for in the base product specification.

- Any proposed alternate systems must be submitted and receive approval 21 days prior to the bid. All post bid submissions will not be considered. This submission shall be in accordance with MATERIALS AND SUBSTITIONS.

- Any manufacture wishing to submit for prior approval must provide the following:

- A working 6 inch sample of the proposed system with a letter describing how the system is considered superior to the specified system.

- A project proposal drawing illustrating the recommended alternate system installed in the application, specific to the project.

- Verifiable list of prior installations showing prior and successful experience with the proposed system.

- Any substitution products not adhering to all specification requirements within, will not be considered.

1.05	Quality Assurance

A.	Manufacturer: Shall be ISO-9001:2000 certified and shall provide written confirmation that a formal Quality Management System and Quality Processes have been adopted in the areas of, (but not limited to) engineering, manufacturing, quality control and customer service for all processes, products and their components. Alternate manufacturers will be considered provided they submit written proof that they are ISO 9001:2000 certified prior to the project bid date. Manufacturers in the process of obtaining certification will not be considered.

B.	Warranty: The expansion control system shall be warranted when installed by the manufacturer’s factory trained installer. Installation shall be in strict accordance with manufacturer’s technical specifications, details, installation instructions and general procedures in effect for normal intended usage and suitable applications under specific design movements and loading conditions.

C.	Manufacturer: Shall have a minimum ten (10) years experience specializing in the design and manufacture of expansion control systems.

D.	Products: Expansion control systems shall be installed with manufacturer’s blockout repair and infill materials.

E.	Application: The specified expansion control system(s) shall be installed by the manufacturer’s factory trained installer.

PART 2 - PRODUCT

2.01	General

A.	The joint seal shall be extruded from a preformed flexible cellular neoprene expanded rubber with a relatively dense layer of skin at the surface and shall be held in place by a two component 100% solids epoxy adhesive.  The design of the seal shall accommodate movements and variations in joint widths through compression and tension of its shape.  Serrated sidewalls shall be extruded to ensure an effective and quality surface for adhesion.

For horizontal and vertical expansion joints furnish Wabo®InverSeal as manufactured by Watson Bowman Acme and as indicated on drawings.  Select appropriate size of profile based on project requirements.

2.02	Materials

A.	Seal Profile - The profile shall be preformed and manufactured from closed cell polychloroprene (neoprene).  The profile shall meet the requirements of the properties listed in the table below unless specified otherwise.

Physical Properties of Wabo®InverSeal

| Property | Requirements | ASTM Method |
| --- | --- | --- |
| Tensile Strength, min. | 125psi | D-412 |
| Elongation Break min. | 200% | D-412 |
| Compression Deflection | 5-9psi | D-1056 |
| Hardness Shore”00” | 35-65 | D-2240 |
| Water Absorption (by weight) | 5% | D-1056 |
| Density (pcf) Average | 12-25 | D-1056 |
| Compression Set (Average %)-1/2” Compressed 50% 22 hrs 70°F - 24hr Recovery | 15-25 | D-1056 |

- Two Component Epoxy Adhesive - The adhesive shall be two-component,  epoxy-based adhesive, which shall have the following properties:

Tensile Strength	4000 PSI

Compressive Strength	8000 PSI

Solids Hardness	5 MOHS

Pot Life	40 minutes at 68°F(20°C)

Flash Point	Greater than 200°F(93°C)

Initial Cure	24 Hours

Full Cure	 7  Days at 68°F

2.03		Fabrication

A.	Seal profiles shall be shipped in the longest practical continuous lengths in manufacturer’s standard shipping carton.  Seals shall be cut to length on jobsite where required. Miter cut or bend seal (depending on size) in the field to conform to directional changes unless otherwise contracted with expansion joint manufacturer.

B.	Epoxy Adhesive will be shipped in manufacturer’s labeled containers.

2.04	Finishes

A.	Seal profile - Supply in color:  Black.

PART 3 - EXECUTION

3.01	Installation

A.	Construction Requirements

- General

- Installation must be performed in gap openings with sound, clean and dry substrates.

- Gap openings must have parallel, dimensionally consistent side walls.

- Any loose portion of concrete at the gap must be removed and the concrete properly repaired as directed by the engineer.

- Concrete (New Construction)

- Forming materials should be carefully removed to avoid edge spalling of the concrete.

- Joint gap edges should be chamfered to help prevent small fractures and spalling.

- Edge spalling conditions should be repaired and allowed to properly cure prior to installation of the Wabo®InverSeal. Repairs shall be made as directed by the Engineer.

- The concrete side walls must be sound and free of all contaminants such as grease, oil, form release agents. etc., prior to installation of the Wabo®InverSeal.

- The preferred method of surface preparation to produce laitence-free, roughened side walls is abrasive blasting. Where abrasive blasting is not permitted, disc grinding will be employed.  Care should be taken to insure that coarse disc is used so as to produce an abraded surface.

- The gap openings should be blown out with clean air to remove dust.

- Concrete (Existing)

- Installation must be performed in gap openings with sound, clean and dry substrates.

- Gap openings must have parallel, dimensionally consistent side walls.

- Any loose portion of concrete at the gap must be removed and the concrete properly repaired as directed by the engineer.

- Steel (New or Existing)

- Steel surfaces must be abrasive blasted immediately prior to installing the Wabo®InverSeal Profile. This is a requirement in new or existing construction. All oxidation must be removed and “white steel” revealed. Where abrasive blasting is not permitted, steel surfaces will be aggressively disc ground to roughen and abrade the surface to achieve the “white steel” condition.

- Stainless steel surfaces require aggressive grinding and abrasive blasting to remove the smooth, glassy surface.

- On galvanized steel surfaces, the galvanizing material must be removed to look like “white steel.”  Careful visual inspection is required because galvanized steel looks like “white steel.”

- Installation of the Wabo®InverSeal Profile into steel should immediately follow abrasive blasting to avoid re-oxidation of the steel surface.

- Wabo®InverSeal Installation

- Prior to installation, the profile shall be uncoiled from shipment packaging and allowed to reach a relaxed condition.

- The Wabo®InverSeal Profile shall be cut to the correct length for installation. Care should be taken to extend the profile to its full length, without exerting any tension.

- The ribbed areas should be aggressively scrubbed with the Profile Conditioning Agent and a stiff nylon brush.

- Following the brush cleaning, the ribbed area shall again be scrubbed using clean, absorbent white cotton rags.

- The two components of the adhesive should be thoroughly mixed until uniformly blended.

- Coat the sidewalls of the joint interface with adhesive starting at the top surface, to a depth equal to the lowest rib of the Wabo®InverSeal.

- The adhesive should then be applied to the profile so that it covers the entire ribbed portion of the profile.

- The profile should then be inserted into the joint gap using a blunt tool to position it to the proper depth.

- Using a clean rag dampened with concrete cleaner, wipe the exposed surface of the Wabo®InverSeal profile.

3.02	Clean and Inspect

A.	Protect system from damage during construction. After work is complete in adjacent areas, clean exposed surfaces with a suitable cleaner that will not harm or attack the seal profile.