Jeene®

# Structural Sealing System

### for Bridge & Highway Applications

A.	General

The work shall consist of furnishing and installing a structural sealing joint system in accordance with the details shown on the plans and the requirements of the specifications.

Manufacturer shall a minimum ten (10) years experience specializing in the design and manufacture of expansion control systems

- Quality Control

Manufacturer shall be ISO-9001:2015 certified and shall provide written confirmation that a formal Quality management System and Quality Processes have been adopted in the areas of, (but not limited to) Engineering, Manufacturing, Quality Control and Customer Service for all processes, products and their components. Alternate manufacturers will be considered provided they submit written proof that they are ISO 9001:2015 certified prior to the project bid date.

# C.	Product

The structural sealing joint system shall be deigned to withstand structural movement and harsh environmental conditions.  The system shall consist of a preformed neoprene profile, installed using the same dimensions as the joint gap at mid-range temperature, bonded with a two component epoxy adhesive and pressurized during the adhesive cure time. Serrated sidewalls shall be extruded to ensure an effective and quality surface for adhesion. Provide seal profile that satisfies project requirements including movement and watertightness. Install all components utilizing manufacturer’s recommended adhesive for complete installation.

# D.	Component and Materials

The Contractor shall furnish a manufacturer’s certification that the materials proposed have been pre-tested and will meet the requirements as set forth in the specification.

1.	Elastomeric Seal

The structural sealing joint profile shall be preformed and manufactured from an extruded neoprene compound exhibiting the physical properties listed in the table below:

Jeene®

# Structural Sealing System

### for Bridge & Highway Applications

PHYSICAL PROPERTIES		TEST METHOD		REQUIREMENT

Tensile Strength			ASTM D412		2000 psi,

Elongation @ break			ASTM D412		250%, min

Hardness, Type A Durometer		ASTM D2240		65  +/-5 % points

Low temp stiffening 7 days @ 14°F				0 - +15

Oven Aging 70 hrs @ 212°F		ASTM D573

Tensile Strength						20% loss max

Elongation							20% loss max

Hardness							0 to +10 points

Oil Swell, 70 hrs @ 212°F (100°C)	ASTM D471		45%

Ozone Resistance,			ASTM D1149		No Cracks

20% strain, 3 PPM in Air

70 hrs @ 104°F (40°C)

- Adhesive

Elastomeric seal shall be installed utilizing a two component epoxy based adhesive which meet the requirements of the properties listed below:

PHYSICAL PROPERTIES		REQUIREMENT

Tensile Strength			3500 to 4000 PSI min.

Compressive Strength			8000 PSI min.

Solids hardness				5 mohs

Pot Life					40 minutes @ 77°F (25°C)

Flash Point				Greater than 150°F (65.5°C)

Tensile Strength, 24 hr			3000 PSI min.

Axial Compression, 24 hr		6500 PSI min.

### E.	Construction Requirements

The Contractor shall submit product information and necessary details after the award of the contract. At the discretion of the Engineer, the manufacturer may be required to furnish a representative sample of material to be supplied in accordance with the project specifications

Where indicated and noted on the contract plans, install structural sealing joint system in a neat and workmanlike manner. All foreign materials and debris which may be detrimental to effectively sealing the joint must be totally removed from the gap. The joint interfaces must be first cleaned by disc grinding or sandblasting and then vacuumed or blown with dry, oil free compressed air before the two component epoxy adhesive is mixed and applied

Jeene®

# Structural Sealing System

### for Bridge & Highway Applications

Pressurization is done through a valve with cap system. The profile is pressurized during installation and curing time of adhesive to assure complete bonding throughout gap/profile surfaces. Air pressure will bleed itself with time or air valve can be released at any time after 24 hours of installation.

Structural sealing joint system shall be set to the proper width for ambient temperature at the time of installation and shall be installed in strict accordance with the manufacturers written instructions along with the advice of their qualified representative.

### F.	Payment

The accepted quantity of structural sealing joint system will be paid for at the contract unit price per lineal foot. Measurement of the structural sealing joint system will be taken horizontally and vertically along the centerline of the joint system between the outer limits indicated on the contract plans. Payment will be made under:

PAY ITEM					PAY UNIT

Structural Sealing Joint System		Lineal Foot

Payment will be full compensation for all work necessary to complete the items including furnishing and installing the structural sealing joint system, and any miscellaneous patching required.